## Slide 1: MRPL Technical Inspection Briefing
Equipment Tag: E-1102 | API 510 Remaining Life Assessment

## Slide 2: Ultrasonic Thickness Inspection (E-1102)
Measured Thickness: 8.4 mm (T_min threshold: 6.5 mm)
Calculated Corrosion Rate: 0.6 mm/year
Remaining Service Life: 3.17 years

## Slide 3: Engineering Directives & Actions
Approved for continuous service under current operating envelope.
Mandatory survey scheduled for Turnaround 2028.